HILEC 540R SERIES

SILICONE RUBBER COATED FIBERGLASS SLEEVING

| THERMAL CLASS: 200C | MIL-I-3190/6 (grade A) |
| --- | --- |
| # NEMA TF-1, TYPE 5 | ASTM D372 |

UL FILE E123956 (grade A)

| DESCRIPTION 540R SERIES is comprised of a two-component liquid silicone rubber continuously applied to premium electrical grade braided fiberglass sleeving. 540R SERIES offers superior coating adhesion to the fiberglass than extruded type products while retaining excellent flexibility and expandability over a wide range of temperatures (-55C to +200C). | #### RECOMMENDED USE # 540 SERIES is used where high temperature requirements are coupled with flexibility, abrasion resistance, moisture resistance, cut-through resistance, expandability and chemical resistance. Typical applications for 540R SERIES include DC motor lead protection, high current dry transformers and automotive under-the-hood wire protection. |
| --- | --- |

PHYSICAL PROPERTIES (coating)

| ### Hardness | 30 durometer, shore A |  | ## Resistance to: Ozone | Excellent |
| --- | --- | --- | --- | --- |
| Tensile Strength | >1000 psi |  | ### Corona | Excellent |
| Elongation | >600 % |  | Radiation | Excellent |
| 100% Modulus | 300 psi |  | Sunlight | Excellent |
| Tear strength | 150 ppi |  | Fungus | Excellent |
| Compression set | >8.0% (22 hrs @ 177C) |  |  |  |

| ##### DIELECTRIC GRADE | ##### PRODUCT NUMBER | MIN. AVE. BREAKDOWN | MIN. INDIV. |
| --- | --- | --- | --- |
| A | ##### 547R | 8000 | 6000 |
| B | 544R | 4000 | 2500 |
| C-1 | 542R | 2500 | 1500 |
| C-2 | 541R | 1000 | 800 |

###### AVAILABILITY # SIZES: 540R SERIES is available in continuous spooled lengths or cut lengths in NEMA sizes #24 through 1”. - COLORS: 540R SERIES is available in black, white, and tan. Other colors may be available subject to minimum order quantities and/or set-up charges. - BRANDNAMES: 540R SERIES is also available as VOL-SIL and SRG 300™.

The above data is informational only and should not be used for specification purposes. 11/01